PRODUCT INFORMATION

Lival Licker Konz

Special product for cleaning and regreasing leathers and silk

- Highly concentrated oil preparation with low-wetting detergent emulsifiers.

- Free from foreign solvents.

- Renews the natural, supple handle of leather-wear and loosens suede pile.

- Suitable as leather licker since it emulsifies with water.

- Regreasing agent washing leather.

- Refreshes colour of silk articles.

Application

For the regreasing as leather licker and the washing of leather and refreshing colour of silk articles.

After-spraying as leather licker for leather articles which were cleaned in perc or hydrocarbon before:

Lival Licker Konz is diluted approx. 1:10 with water and stirred well.   It is recommend to place the water first and then to add Lival Licker Konz stirring all the time.   Apply approx. 250ml of the licker emulsion per leather item uniformly with a spray gun.   The leather should be moistened regularly.   Soaking through to the leather does not have negative effects provided normal colour fastness.

The treated items are air dried for approx. 30-60 minutes first, afterwards they are tumbled.   By tumbling the items the fat is levelled.

For velour leather an artificial leather sponge has to be added into the tumbler.   This will intensify the brilliance of colours and the chalking effect.

Additional hint for an improvement of the impregnation:

The following method is proven to be of good effect:   4 parts water are placed first, 1 part Lival Licker Konz and 5 parts Lival VLF are added while stirring all the time.   The resulting spray solution will have a colour-intensifying, a regreasing and at the same time an impregnating effect.   The solution tends to separation, it has to be shaken or stirred from time to time.

Washing leather apply as follows:

After rinsing and slight centrifuging Lival Licker Konz is added at low liquor lever at 20-30 degrees C.

Applied quantities

Approx. 10-30 ml/kg or approx. 3-10 ml/l water

Treat the textiles for approx. 5 minutes, then centrifuge in intervals and hang for drying.   The seams have to be pulled.   Wrinkles of centrifuging and marks of the drum should be removed in advance.   After drying the items can be loosened in the tumbler.

Treating silk articles apply as follows:

Single silk articles are treated for regreasing and refreshing of colours by the manual dipping method.   Mix thoroughly approx. 100ml Lival Licker Konz and 10 1 tap water – placing the water first.

The silk articles are moved by hands carefully for 1-2 minutes in this solution.   Take them off, after possible slight centrifuging or rolling into a towel hang them for drying.

The treated items are finished after drying in accordance with the normal process employed by the applicant.

0800 074 2325

www.textile-care.co.uk

sale@textile-care.co.uk